TITANIUM DIOXIDE

R-606

RUTILE PIGMENT

Applications:

R-606 is a universal pigment with superior exterior and interior durability.  It is designed to provide excellent dispersibility, high opacity, and high gloss.  R-606 is well suited for use in paint & coatings, inks, and plastics.

Standards:

TiO2 Content                                				  ≥ 93.0%

Retained on 325 Mesh		                                  ≤ 1.0%

Oil Absorption                                                                 ≤ 22 g/100g

pH								     6.5 – 8.5

Soluble matter in water					  ≤ 0.5%

Volatile content @ 105° C                                               ≤ 1.0%

Resistivity			                        		   ≥ 120.0 Ω∙m

Rutile content of TiO2                                                       ≥ 98.0%

CIE L*								   ≥ 98.0

CIE b*								   ≤ 2.5

Surface Treatments:	Zirconium and Aluminum

Classification:		ISO 591-1:  2000		R2

CAS No.:	13463-67-7

Packaging:	25 kg (55.12 lb.) woven plastic bags

1000 kg (2,204.6 lb.) super sacks